## Slide 1
SPIN Qubits
in Quantum dots
Covering: basic concepts, measurement techniques, implementations, qubit approaches, current trends
With figures and slides borrowed from
L. Vandersypen, J. Elzerman, R. Hanson, L. Kouwenhoven, M. Veldhorst (TU Delft)

## Slide 2
Initialization 1-electron, low T, high B0
Loss & DiVincenzo, PRA 1998 Vandersypen et al., Proc. MQC02 (quant-ph/0207059)
H0 ~ S wi szi
Coherence long relaxation time T1 long coherence time T2
ESR pulsed microwave magnetic field
HRF ~ S Ai(t) cos(wi t) sxi
SWAP exchange interaction
HJ ~ S Jij (t) si · sj
Read-out convert spin to charge
then measure charge


Spin qubits in quantum dots
SL
SR

## Slide 3
IQPC
DRAIN
SOURCE
RESERVOIR
G
200 nm
M
P
R
Q
T
Vandersypen et al, APL 2004
See single electrons jump on/off the dot in real-time
Real-time single-electron detection
VSD = 1 mV
IQPC ~ 30 nA
∆IQPC ~ 0.3 nA
Shortest steps ~ 8 µs
3

## Slide 4
response
to pulse
DIQPC (nA)
Time (ms)
0
0.5
1.0
1.5
response
to electron
tunneling
0.0
0.4
0.8
-0.4
Pulse-induced tunneling
4

## Slide 5: Energy-selective readout
~G -1
0
-e
Q
time
0
-e
Q
time
‘up’
‘down’
and
split due to
high magnetic field


Elzermann et al., Nature (‘04)
5

## Slide 6: Energy-selective readout
~G -1
0
-e
Q
time
0
-e
Q
time
Limitations:
Requires ΔEZ >> kBT
Sensitive to background charge fluctuations (“switching”)
Sensitive to HF noise (photon-assisted tunneling)
Elzermann et al., Nature (‘04)
6

## Slide 7: Readout pulse scheme
DRAIN
P
V
(
m
V
)
time
inject & wait
read-out
empty
empty
10
5
0
DI
Q
P
C
time
in
Q
dot
= -
e
Q
dot
=0
out
Q
dot
=0
out
in
IQPC
DRAIN
SOURCE
RESERVOIR
G
Elzermann et al., Nature (‘04)
7

## Slide 8: Readout pulse scheme
DRAIN
P
V
(
m
V
)
time
inject & wait
read-out
empty
empty
10
5
0
DI
Q
P
C
time
in
Q
dot
= -
e
Q
dot
=0
out
Q
dot
=0
out
in
IQPC
DRAIN
SOURCE
RESERVOIR
G
“SPIN UP”
“SPIN DOWN”
0
1.0
0.5
DIQPC (nA)
0
1
2
1.5
0
1.0
0.5
1.5
Elzermann et al., Nature (‘04)
8

## Slide 9
Energy dissipated in phonon bath
Electric field from phonons couples to spin via spin-orbit coupling
Elzerman et al., Nature 2004 Amasha et al., PRL 2008
Spin relaxation in quantum dots
GaAs
T1’s are over 1 sec at low B
Waiting time (ms)
Spin down fraction
9

## Slide 10
I(nA)
0.3
-10
-5
0
5
-0.2
-0.1
0.0
0.1
0.2
V(mV)
Ono, Austing, Tokura, Tarucha, Science (’02)
S(0,2)
T(0,2)
S(0,2)
T(0,2)
Probe: spin blockade due to Pauli exclusion
10

## Slide 11
Probe: spin blockade due to Pauli exclusion
11

## Slide 12
Initialization 1-electron, low T, high B0
Loss & DiVincenzo, PRA 1998 Vandersypen et al., Proc. MQC02 (quant-ph/0207059)
H0 ~ S wi szi
Coherence long relaxation time T1 long coherence time T2
ESR pulsed microwave magnetic field
HRF ~ S Ai(t) cos(wi t) sxi
SWAP exchange interaction
HJ ~ S Jij (t) si · sj
Read-out convert spin to charge
then measure charge


Spin qubits in quantum dots
SL
SR

## Slide 13
I
CPS
0.3 m
Detection and pulse scheme
13

## Slide 14
Electron Spin Resonance Spectroscopy
14

## Slide 15
Coherent control of a single electron spin
15

## Slide 16
Dot current (fA)
max B1 ~ 1.9 mT, compare BN,z ~ 1.3 mT Analysis: Koppens, Klauser, et al, PRL 2007
Koppens et al. Nature (’06)
1000
0
12
7
0
3.5
fRabi (MHz)
stripline current (mA)
up to 8 periods observed π/2 rotation in 25ns
Burst time (ns)
RF Power (dBm)
0
500
1000
-18
-6
-12
Idot (fA)
Coherent control of a single electron spin
16

## Slide 17
Koppens et al. Nature 2006
BDC

BAC
W
W
250 μm
Veldhorst et al, Nature Nano 2014
GaAs
28Si
Coherent control of a single electron spin
17

## Slide 18
Theory: Golovach et al., PRB (’06)
Rashba
Dresselhaus
Bext // E(t) // [110]
Nowack et al., Science (’07)
Mechanism: spin-orbit interaction
18

## Slide 19
Magnetic field gradient (microfabricated ferromagnet)
Pioro-Ladriere et al, arXiv:0805.1083
Nuclear field gradient (incoherent only)
Laird et al., PRL (’07)
Other mechanisms for electrical driving
19

## Slide 20
Initialization 1-electron, low T, high B0
Loss & DiVincenzo, PRA 1998 Vandersypen et al., Proc. MQC02 (quant-ph/0207059)
H0 ~ S wi szi
Coherence long relaxation time T1 long coherence time T2
ESR pulsed microwave magnetic field
HRF ~ S Ai(t) cos(wi t) sxi
SWAP exchange interaction
HJ ~ S Jij (t) si · sj
Read-out convert spin to charge
then measure charge


Spin qubits in quantum dots
SL
SR

## Slide 21
Petta et al., Science 2005
swap1/2 in as little as 180 ps
Dial et al., PRL 2013
Wu et al., PNAS 2014
Gate voltage pulse controls spin exchange
Decay from charge noise
Coherent exchange of two spins
21

## Slide 22
Coherent exchange of two spins
D. Loss and D. P. DiVincenzo
Phys. Rev. A 57, 120 (1998)

## Slide 23
Martins et al, PRL 2016, see also Reed et al, PRL 2016
Operation at the symmetry point
23

## Slide 24
Xiao Xue, et al., Nature 601, 343 (2022)
‘Now that the 99% barrier for the two-qubit gate fidelity has been surpassed, semiconductor qubits have gained credibility as a leading platform, not only for scaling but also for high-fidelity control.’
Y. Noiri, et al. Nature 601, 338 (2022)
Computing with spin qubits at the surface code error threshold
24

## Slide 25
Initialization 1-electron, low T, high B0
Loss & DiVincenzo, PRA 1998 Vandersypen et al., Proc. MQC02 (quant-ph/0207059)
H0 ~ S wi szi
Coherence long relaxation time T1 long coherence time T2
ESR pulsed microwave magnetic field
HRF ~ S Ai(t) cos(wi t) sxi
SWAP exchange interaction
HJ ~ S Jij (t) si · sj
Read-out convert spin to charge
then measure charge


Spin qubits in quantum dots
SL
SR

## Slide 26
Overhauser field BN
Full polarization
GaAs: A ~ 5.5 T
Paget, 1977
Statistical polarization
GaAs dot: N ~ 106
BN = A / N1/2 ~ 5 mT
Merkulov, Efros, Rosen, PRB 2002
Khaetskii, Loss, Glazman, PRL 2002
Nuclear correlation time
GaAs: ~ 100 ms - few sec.
Hyperfine interaction with the nuclear spins
26

## Slide 27
GaAs
T2* ~ 10 ns
Petta et al,
Science 2005
Bluhm et al.,
Nat Phys 2008
T2CPMG ~ 0.2 ms
Si
T2* ~ 1 ms
Kawakami, Scarlino, et al,
Nature Nano 2014
T2CPMG ~ 0.5 ms
28Si
T2* ~ 100-250 ms
Veldhorst, et al,
Nature Nano 2014
T2CPMG ~ 28-500 ms
Muhonen et al,
Nature Nano 2014
Trend 1: Eliminate nuclear spins
Pulse toolbox
Dynamical decoupling
Ramsey
CPMG
Hahn echo
New kid on the block: Ge
Hendrickx et al, Nature 577, 487 (2020)
27

## Slide 28
Coherent spins in isotopically purified silicon
For electron spin:
T2*= 200us
T2 = 28ms
FC = 99.9%
Veldhorst, et al. Nat. Nanotech 9, 981 (2014)
Yoneda, et al. Nat. Nanotech 13, 102 (2018)
Si-natural
Si-purified
GaAs
Trend 1: Eliminate nuclear spins
In Si28 epilayer (Si-SiOx)
In Si28 quantum well (SiGe)
28

## Slide 29
Two-qubit devices for electrons in silicon
28SiMOS
SiGe
SiGe
Veldhorst et al., Nature 526, 410 (2015)
Watson et al., Nature 555, 633 (2018)
Zajac et al., Science 359, 439 (2018)
Xiao Xue, et al., Nature 601, 343 (2022)
Y. Noiri, et al. Nature 601, 338 (2022)
Computing with spin qubits at the surface code error threshold
‘Now that the 99% barrier for the two-qubit gate fidelity has been surpassed, semiconductor qubits have gained credibility as a leading platform, not only for scaling but also for high-fidelity control.’
Trend 1: Eliminate nuclear spins
29

## Slide 30: Pulse scheme to measure T1
GT ~ 50 kHz; GS ~ 2.5 kHz
QPC bandwidth ~ 20 kHz
time
V
P
V
(
m
V
)
time
inject & wait
read-out
empty
empty
10
5
0
DI
I
Q
P
C
in
Q
dot
= -
e
Q
dot
=0
out
Q
dot
=0
out
in
IQPC
RESERVOIR
G
200 nm
Elzermann et al.,Nature (‘04)
“SPIN UP”
“SPIN DOWN”
30
Notes: presence or absence of an electron

## Slide 31: Pulse scheme to measure T1
GT ~ 50 kHz; GS ~ 2.5 kHz
QPC bandwidth ~ 20 kHz
time
V
P
V
(
m
V
)
time
inject & wait
read-out
empty
empty
10
5
0
DI
I
Q
P
C
in
Q
dot
= -
e
Q
dot
=0
out
Q
dot
=0
out
in
IQPC
RESERVOIR
G
200 nm
~1/T1
Elzermann et al.,Nature (‘04)
“SPIN UP”
“SPIN DOWN”
DIQPC (nA)
Time (ms)
Time (ms)
0
1.0
0.5
0
1
2
1.5
0
1.0
0.5
1.5
‘up’
‘down’
timescale: 100 μs up to > 1 s (!)
Notes: presence or absence of an electron

## Slide 32: Environment and interactions in GaAs
+
-
Spin-orbit coupling
Uncontrolled electric fields
- phonons
Absorb the energy, but conserve spin.
Admixes pure spin states.
32
Notes: It is meanwhile established, that

## Slide 33: Spin-orbit coupling in hydrogen
+
-
+
-
Hydrogen atom
Rest frame electron
In hydrogen:
33

## Slide 34: Spin-Orbit coupling in a crystal
-
Crystal symmetry determines the geometry of the electric field the electron ‘sees’
Zincblende structure has no inversion symmetry (Bulk Inversion Asymmetry)
Due to low symmetry electric fields don’t cancel out
34

## Slide 35: Spin-Orbit coupling in a two-dimensional electron gas
-
Rashba
Dresselhaus
Structure given by symmetry, microscopic details of the atomic structure hidden in the coupling strength
x|| [100]
y||[010]
Experiments in 2D: e.g. Kato et al., Nature (’03),
Meier et al., Nature Physics (’08)
Notes: Band structure calculations…
Symmetry arguments…
Effect of confinement potential of the two-dimensional electron gas…
That is something observed in experiments in 2D systems, where the spin of a propagating electron precesses aroudn the internal magnetic field.

## Slide 36
Spin-orbit coupling in a quantum dot
36

## Slide 37: Spin-orbit coupling and uncontrolled electric fields
B^5 dependence
Uncontrolled electric fields
- phonons
x
y
z
Bext
electric fields couple to the electron position:
37

## Slide 38: Spin-orbit coupling and uncontrolled electric fields
B^5 dependence
Uncontrolled electric fields
- phonons
­
¯
x
y
z
Bext
38
Notes: …which couples transition to transitions from up to down

## Slide 39: Spin-orbit coupling and uncontrolled electric fields
B^5 dependence
Uncontrolled electric fields
- phonons
­
¯
depends linearly on external field
phonon density of states at Zeeman
splitting
dot – phonon coupling
electric field amplitude
B5
dependence

## Slide 40: Spin-orbit coupling combined with controlled electric fields
x
y
z
Bext
Excite a local gate!
+
DC
­
¯
­
¯
40
Notes: Wait… What about controlled electric fields

## Slide 41: Detection and pulse scheme
(1) Pauli exclusion: no two electrons in same state
(2) Spin selection rule: transition is spin-conserving
Ono et al. Science (’02)
Johnson et al. PRB (’05)
Koppens et al. Nature (‘06)
Reminder
I
CPS
41

## Slide 42: Electrically driven Rabi oscillations
fAC=15.2GHz
Rabi frequency depends linear on electric field amplitude
fAC=14GHz
Nowack et al., Science (‘07)
42

## Slide 43
Trend 2: Scaling up tunnel coupled arrays
C. Volk, A-M. Zwerver et al, npj Q Info 2019
A.R. Mills et al, Nature Comm 2019
Mukhopadhyay, Dehollain et al. APL 2018
Mortemousque et al, arXiv:1808.06180
43

## Slide 44
Vision of a scalable spin qubit architecture
Local registers
Quantum links
Integrated electronics
Using the strengths of spin qubits: “Hot, dense and coherent” Vandersypen et al., npj Q Info 2017
44

## Slide 45
Samkharadze, Zheng, et al., Science 2018 X. Mi et al., Nature 2018 Landig, Koski, et al., Nature 2018
Strong spin-photon coupling
Trifunovic et al, PRX 2012
Shulman et al, Science 2015
Capacitive coupling
Trend 3: Distant coupling of spin qubits
Fujita et al, npj Q Info 2017 Flentje et al, Nature Comm 2017
Spin shuttles
45

## Slide 46: Quantum Dot - Cavity Hybrid Technology
Building a coherent interface for hybrid technology
via high impedance resonators
Superconducting circuits platform
Semiconductor QDs platform
Hybrid QD-resonator devices
For investigating light-matter interaction at the fundamental level and implementing a rich set of novel applications in quantum information technology
While both superconducting and semiconducting platforms have strong potential for quantum technology on their own, we will explore novel opportunities emerging at the interface between the two hardware.
46

## Slide 47
Circuit QED architecture: coherent link
Circuit Quantum Electrodynamics
Strong coupling of the qubit to a quantum information mediator (photon)
Interaction of distant qubits
Raimond et al., Rev Mod Phys 73, 565 (2001)
Haroche & Raimond, OUP Oxford (2006)
Ye et al., Science 320, 1734 (2008)
Blais et al., Phys Rev A 69, 062320 (2004)
Wallraff et al., Nature 431, 162 (2004)
Schoelkopf & Girvin, Nature 451, 664 (2008)
electron charge
electron spin
Quantum Dot - Cavity Hybrid Technology
47

## Slide 48
Integrated GaAs DQD with SQUID Array Resonator in Hybrid Device
Stockklauser*, Scarlino* et al., PRX 7, 011030 (2017)
Microwave reflectometry measurement
Josephson parametric amplifier
Custom FPGA electronics
32 SQUID array resonator
long
Al based
Dolan bridge technique
Gate defined GaAs DQD
On small mesa
Resonator coupling gate not DC biased
Quantum Dot - Cavity Hybrid Technology
48

## Slide 49
    Qubit is very sensitive to litho variations, scattering, defects, charge noise and even nuclear spins
SiGe barrier
Si q well
Challenge: Qubits have personalities
49

## Slide 50
10 years, 50 M$
Silicon spin qubits
Transmon qubits
Architecture, Cryo-CMOS,
Interconnects
Transistor: 1 gate / 1 device
QDots: 2N+3 gates / N devices
Quantum dots made @ Intel 300 mm cleanroom
Trend 4: Qubits made by advanced semiconductor manufacturing
QuTech-Intel collaboration
arXiv:2101.12650
50

## Slide 51
51

## Slide 52
Why did it take 10 years for Silicon?
(Effective mass) m*//=0.2 for Si, m*=0.067 in GaAs
Fabrication issues lattice mismatch, defects, failing contacts, leaky gates
Noisy substrates
Valley degree of freedom
4.2%
mismatch
52

## Slide 53: Valley splitting in silicon
  Zwanenburg et al, Rev. Mod. Phys. 85, 961 (2013)
Eorb
Evalley
53

## Slide 54
Coherence
Manipulation
Relaxation (T1)
Decoherence (T2)
Single- and two-qubit gates
Long-distance coupling
Individual addressability
Ge: 92.2 %
Spin-orbit switch
Si: 95.3 %
High mobility
No valley degeneracy
Suppressed Hyperfine interaction
Mostly nuclear spin zero
More advantages:
Strong spin-orbit interaction
Tunable strength
Tunable g-factor/qubit energy
Trend 5: Holes’ spins in Germanium
54

## Slide 55: Review articles
Introduction to spin qubits:
  Vandersypen and Eriksson, Physics Today 72, 8, 38 (2019)
Single dots:
  Kouwenhoven et al, Rep. Progr. Phys. 64 (6), 701 (2001)
Double dots:
  van der Wiel et al., Rev. Mod. Phys. 75, 1 (2003)
Spins in dots
  Hanson et al, Rev. Mod. Phys. 79, 1217 (2007)
Spin qubits in silicon
  Zwanenburg et al, Rev. Mod. Phys. 85, 961 (2013)
Scaling spin qubits
  Vandersypen et al, npj Q Info 3, 34 (2017)
55